
Aqua Clear B – Resin is a 100% reactive low viscosity liquid bisphenol-A based epoxy resin diluted with an Alkyl glycidyl ether.  This resin is specially designed for applications requiring low viscosity, minimum odor and good color.

Typical Properties:



Epoxide Equivalent Wght 
  ASTM D1652
  q/eq

195 – 215




Viscosity @ 25 degrees C
   ASTM D445

    P

    5 – 7


Color 


              ASTM D1544
  Gardner
1 max.




Physical Form







Clear Liquid




Pounds per gallon @ 25 degrees C


  1bs/gal
9.2    



Density @ 25 degrees C



  q/ml

1.1




Flash Point 


   ASTM D93

  F

>240




Specific Heat





  BTU/lb
0.45




_______________________________________________________________

Performance Properties:


Units

PERFORMANCE


Aqua Clear B


pbw - 100


Handling Properties







Pot Life ½ pint

minutes


136




Initial Viscosity

cP



460




Cure Schedule

Hours/ F

     4/77+2/302



Tensile Properties @ 25 C






Ultimate Strength

psi



7.800




Ultimate Elongation

%



5.3




Modulus


ksi



410



Flexural Properties, @ 25 C





Strength


psi


          14,000




Modulus


ksi



420



Tg by DSC



C (F)



77 (171



Chamical Resistance, % by wght gain




Acetone, 3 hrs @ 56 C
%



0.5




Water, 24 hrs @ 93 C
%



3.0

[image: image1.jpg]ASTE
PACK




32302 Camino Capistrano #201, San Juan Capistrano, CA 92675 – (949) 487-2068 – Fax (949) 487-2312

sales@masterpkg.com – www.MASTERPKG.com
TECHNICAL DATA SHEET


  AQUA CLEAR – COMP B – RESIN





							  	      Rev. 9/30/06








Property		Test Method	Unit		Value








