[image: image1.jpg]ASTE
PACK





32302 Camino Capistrano #201

(949) 487-2068 – Fax: (49) 487-2312
San Juan Capistrano, CA 92675


PRODUCT INFORMATION:
Master Pack 1420-0.5 is a two component, water blown, polyurethane open cell spray foam system. The in-place density is 0.5 lbs/ft3. Low viscosity and 1:1 by volume ratio provide for easy processing. The foam is rated CLASS I according to ASTM E 84 at four inches.

USES:
Master Pack 1420-0.5 is designed for use in applications such as Insulation Foams, Sound Deadening, and Void Fill ECT.

REACTIVITY PROFILES:







REGULAR




                            











CURED FOAMS TYPICAL PHYSICAL PROPERTIES

(DATA DERIVED FROM LABORATORY SAMPLES)


      

    



PROCESSING GUIDE

STORAGE/SHELF LIFE. Components “A” and “B” should be stored in their original,

unopened containers at temperatures between 55°F and 85°F. Shelf life of unopened, sealed containers is approximately six months under those storage conditions.

EQUIPMENT. Recommended proportioning equipment is manufactured by Gusmer, Binks, Graco, or Glas-Craft. Mixing and ratio by volume is 50 parts A to 50 parts B (1:1). Equipment shall be of the heated, airless type, capable of maintaining 100°F to 130°F at the spray gun. Optimum spraying temperature will vary with type of equipment used, substrate, ambient temperature, and humidity.

WARNING: Polyurethane foam may present a fire risk in certain applications if exposed to fire or excessive heat, e.g. welding and cutting torches. The use of polyurethane in interior applications on walls or ceilings presents an unreasonable fire risk, unless the foam is protected by an approved fire-resistive fifteen-minute thermal barrier.

GENERAL INSTRUCTIONS. Before the containers are opened, all safety instructions should be read and understood by all personnel who will come into contact with the materials. If the safety instructions are lost or otherwise not available, please contact Master Pack for a replacement. A Master Pack Material Safety Data Sheet (MSDS) is sent with the original shipment and available upon request. All personnel who come in contact with the product should read and understand the MSDS.

PROTECTIVE EQUIPMENT. The “A” component is a polymeric isocyanate and may be sensitizing, particularly from the standpoint of VAPOR INHALATION. The best form of protection against sensitizing vapors in the workplace is a FRESH AIR SUPPLY. Several manufacturers, including 3M company and MSA make full face fresh air masks. For minimum protection, organic vapor canister style respirators shall be worn. To prevent contact with the product, wear fabric coveralls and fabric gloves, full-face mask and OSHA approved protective goggles.

HEALTH AND SAFETY
VAPOR INHALATION problems are characterized by coughing, shortness of breath or

tightness of the chest. Anyone exhibiting these symptoms shall be immediately removed from the workplace and administered oxygen or fresh air. If the condition is prolonged or extreme, SUMMON “EMERGENCY TRAINED” MEDICAL ATTENTION IMMEDIATELY.

SKIN CONTACT with liquid components can result in a rash or other irritation. Wash the affected area with water. Wipe residual liquid with a clean soft cloth followed by washing with soap and water. If a rash or other irritation develops, SEE A PHYSICIAN.

EYE CONTACT with liquid or sprayed components can result in corneal burns or abrasions. Upon exposure, eyes should be flushed with water for an extensive period. SUMMON “EMERGENCY TRAINED” MEDICAL ATTENTION IMMEDIATELY.

WARNING:

Polyurethane products manufactured or produced from these chemicals may present a serious fire hazard if improperly used or allowed to remain exposed or unprotected. The character and magnitude of any such hazard will depend on a broad range of factors which are controlled or influenced by the manufacturer, applicator or production process. Each person, firm, or corporation engaged in the manufacture, production, application, installation or use of any polyurethane materials should carefully determine whether there is a potential fire hazard associated with such specified usage, and utilize all appropriate precautionary and safety measures as outlined in Local, State and Federal regulations governing the manufacture of products or the construction and/or renovation of commercial or residential structures.

















              REGULAR


                       R





	      FAST


                       F





Ambient Temp.


	Range





70 degrees F Min





               40° F Min.





ASTM D-1940








          	   >93 %








Reactivity


(Rise Time)








4 – 6 sec.





2 – 4 sec.





LIQUID


COMPONENTS





   TEST METHOD





COMPONENT 


            A





COMPONENT


             B





Viscosity, cps @ 74°F	


cps





ASTM -2196


Spindle #2 @ 300


rpm





200 + / - 50





250 + / - 100











                  

















Specific Gravity @


74°F


	





ASTM D-1638 





1.24 





1.08








             Visual





      Dark brown	





     Light brown





Color





Weight per gallon





From Specific 


Gravity





          10.33





	8.90





        PROPERTY	





TEST


METHOD





RESULTS





          Density





ASTM D-1622 





     0.5 pcf





Compressive  


Strength


Parallel





ASTM D-1621








                       .95 psi





   K Factor


Initial Rvalue,                   initial	





ASTM C-518


Calculated





0.294


3.4


                             





Tensile


Strength				








ASTM D-1623





4psi





Open cell


Content





Dimensional	  Stability





ASTM D-2126





	+4% max





Moisture


(Perm/Inch)			


(Perm/Inch)





ASTM E-96





15.98 perm


in





THE INFORMATION HEREIN IS BELIEVED TO BE RELIABLE, BUT UNKNOWN RISKS MAY BE PRESENT. Master Pack WARRANTS ONLY THAT THE MATERIALS SHALL BE OF MERCHANTABLE QUALITY; THIS WARRANTY IS IN LIEU OF ALL OTHER WRITTEN OR UNWRITTEN EXPRESSED OR IMPLIED WARRANTIES AND Master Pack EXPRESSLY DISCLAIMS ANY WARRANTY OF FITNESS FOR A PARTICULAR PURPOSE, OR FREEDOM FROM PATENT INFRINGEMENT. ACCORDINGLY, BUYER ASSUMES ALL RISKS WHATSOEVER AS TO THE USE OF THESE MATERIALS. BUYER’S EXCLUSIVE REMEDY AS TO ANY BREACH OF WARRANTY OR NEGLIGENCE CLAIM SHALL BE LIMITED TO THE PURCHASE PRICE OF THE MATERIALS. FAILURE TO STRICTLY ADHERE TO RECOMMENDED PROCEDURES SHALL  RELIEVE Master Pack OF ALL LIABILITY WITH RESPECT TO THE MATERIALS OR THE USE THEREOF.








